## Slide 1: Prosjekt-oppdatering
17.09.2024

## Slide 2: Generating EIS Simulation
Assumptions:
  DFN model
  Same parameters as Amund used in the MJ01 cell
  Input parameter SOC = 45%
    Then used pybamm-eis example to calculate the initial concentration in the positive and negative electrode (updating these parameters)
  25 degrees Celcius
  Applying an AC current!
    Sinus current applied in the time domain =
    Using a numerical frequency domain method (I used prebicgstab)
    Have included a plot where I compare these methods
  Did not include the option: surface integral to generate the semicircle.

## Slide 3: Comparing exp. and sim. Nyquist plot
Observations:
Basically the same if you apply a sinus curve in the time domain or use a numerical method in the frequency domain! Takes shorter time with the latter.
Same ish angle? Simulation shifted to the right? What do you think? Road ahead?

## Slide 4: MJ02 Bode plot
Comments:
Have not found out how I can extract magnitude and phase data from the simulation (and generate Bode plot from this)
Used the same frequency range in the simulation!